# Utilizing Timber Waste as Building Material

# ABSTRACT

This project proposes a design-to-fabrication workflow for producing structural prototypes from timber waste through the combined development of wood-wood joinery, computational placement, and physical testing. Building from the Spruce Beetle workflow developed by Reisach et al., this thesis shifts focus from complex arch-based demonstrators toward simpler, more controllable structural test cases, beginning with planar arches and extending toward compression-oriented column assemblies. The research investigates a set of timber-only joint geometries, ranging from baseline floating tenon configurations to dovetail-inspired and multi-sided column joints, and tests how joint quantity, geometry, and material variation affect fabrication practicality and structural behavior across engineered and irregular waste streams. A parallel goal is extending the existing Grasshopper plugin to generate more complex volumetric geometries like columns and walls and even beams with multi sided joints. The expected contributions include a structured joint comparison, a fabrication and testing methodology for offcut-based prototypes, and tested directions for plugin development.

# INTRODUCTION

Wood waste is abundant in shops, jobsites, and manufacturing environments, and the scale is enormous: 488 million m³ of sawn wood are produced globally, while construction and demolition wood waste alone reaches 11.9 million tons in Germany and 2.31 million tons in Australia (Ilgın & Karjalainen, 2021; Jahan & Zhang, 2022). Even within a single manufacturing stream, timber offcuts can accumulate rapidly. One company documented by Reisach et al. generated up to 12,000 m³ of offcuts per year, underscoring that this is not a marginal byproduct but a substantial secondary resource (Reisach et al., 2024).

Yet much of this material does not remain in high-value use. Current cascading systems apply to only about one fifth of timber, and the EU timber industry is reported to incinerate up to 80% of its waste wood, including offcuts (Reisach et al., 2024). This matters structurally and environmentally: cascading wood use can cut global warming potential by 7% and save up to 14% of annual primary wood supply in modeled systems, while each cubic meter of growing wood binds approximately one ton of CO2 (Höglmeier et al., 2015; Ilgın & Karjalainen, 2021).

Digital fabrication and computational design are beginning to make irregular timber pieces treatable as individually managed, data-driven building elements rather than waste. However, the field remains early. Research on construction and demolition wood waste circularity is still described as scarce across life-cycle stages, regional circular-economy adoption remains underexplored, and missing standards and design guidelines continue to limit widespread implementation of timber connection systems (Arsova & Genovese, 2022; Dissanayake & Gunawardena, 2025; Jahan & Zhang, 2022).

## Research problem

Reisach et al., established an important proof of concept through the Spruce Beetle workflow by showing that short timber offcuts can be digitally selected, placed, jointed, and fabricated into load-bearing demonstrators at full scale (Reisach et al., 2023, 2024). That contribution is significant because it moves timber offcuts beyond immediate incineration or low-value reuse and positions them as a resource that can improve material efficiency and reduce demand for new wood (Reisach et al., 2024; Höglmeier et al., 2015; Mair-Bauernfeind et al., 2017).

However, the main unresolved issue is whether a practical and repeatable process can be built around this “waste”. The current workflow places offcuts along lines or curves and generates joints and fabrication data for those specific arrangements (Reisach et al., 2024). This is a meaningful advance, but broader research on digital timber fabrication suggests that wider adoption depends on better integration with fabrication constraints, more adaptable joint options, and manufacturing methods that reduce manual correction (Ganeshan et al., 2025; Gamerro et al., 2020). Research also shows that digitally fabricated timber joints are highly sensitive to geometry, fit, and material behavior, which means joint selection cannot be treated as an afterthought (Tannert et al., 2016; Gamerro et al., 2020; Moradei et al., 2018).

A second barrier is the limited physical testing behind offcut assemblies intended for structural use. Novel timber connections still face missing design guidelines and significant testing requirements before wider adoption is realistic (Dissanayake & Gunawardena, 2025; Han et al., 2023). This matters especially for offcut systems, because wood-wood connections can vary considerably in stiffness, failure mode, and load behavior depending on geometry, material irregularity, and how force is applied (Rebstock et al., 2015; Han et al., 2023). A credible offcut workflow therefore needs to be developed alongside systematic physical testing that connects joint design to structural performance and fabrication practicality (Gamerro et al., 2020; Han et al., 2023).

The central question is not simply whether timber offcuts can form free standing assemblies, but how a computationally assisted workflow can take advantage of these irregular short waste pieces and turn them into assemblies that are repeatable to produce, straightforward to test, and realistic to scale within circular construction practice (Reisach et al., 2024; Buren et al., 2016).

## Research questions

These gaps lead to the following research questions:

- What combination of joint strategy and computational workflow is sufficient to make offcut-based structural assemblies repeatable and scalable?

- How does joint geometry, count, and spacing affect structural behavior and fabrication practicality in compression-oriented offcut assemblies?

- How can the Spruce Beetle plugin be extended to support joint variation, volumetric geometries like column assemblies, and fabrication planning beyond the baseline arch workflow?

## Thesis direction and scope

Rather than beginning with the complex compound arches used in the ETH demonstrator, this thesis will start with simple planar arches as a controlled first test case and then extend toward compression-focused column assemblies. Planar arches introduce fewer geometric variables, making structural behavior easier to observe and compare while the digital workflow is still being extended. Columns then allow the research to investigate compression behavior, material variability, and scale in a more direct way.

The project retains the broader goals of circularity, material reuse, and data-driven treatment of non-standard material, but prioritizes structural clarity and experimental validation over geometric complexity. The intention is a sequence of increasingly demanding test cases, where findings from each iteration can directly inform the next.

## Research criteria

The proposed work should loosely meet the following criteria:

- recyclable wood-to-wood connections

- no metal fasteners within the primary joint logic

- no adhesive within the primary joint logic

- simple assembly

- compatibility with 3 axis CNC fabrication

- adaptability to irregular or short timber offcuts

- scalability from small specimens to larger demonstrators

- applicability to engineered wood waste streams

- structural usefulness under compression

# ETH CASE STUDY AND RESEARCH GAPS

The ETH case study provides several direct openings for further work.

## Validation and testing

The paper argues for more and larger specimens to improve statistical significance, and it identifies finite element analysis and bending tests as important missing pieces. The published testing focused on tension parallel to grain and shear behavior of loose spline joints, but bending was not completed because of limited resources. For this thesis, that gap supports a stronger testing agenda built around repeatable specimens, simplified structural assemblies, compression-focused prototypes, and additional joint comparisons.

## Joint design refinement

The study found that increasing the number of inserted joint elements improved force distribution and stiffness, and it recommended at least two floating tenon-type connectors per connection and preferably three or four for larger assemblies. It also suggested that joint size should scale with component size.

## Fabrication speed and scalability

The paper reports very slow fabrication times for prototypes and demonstrators, indicating that the current workflow is not yet scalable. This creates a useful thesis opportunity: fabrication can become a research variable rather than just a production step.

## Material capture and digitization

The authors note the challenge of cataloging and managing large quantities of unique offcuts. They discuss manual measurement, photogrammetry, laser scanning, and computer vision as possible pathways. This aligns directly with a practical workflow question: what level of digitization is actually necessary for structurally useful assemblies?

## Standards and certification

The paper emphasizes that no certification system currently exists for waste wood and suggests that structural redundancy and simpler typologies may be appropriate until better assessment methods are available. This further supports a shift toward simpler test structures, where geometry and loading conditions are easier to isolate, interpret, and compare.

# METHODS

The thesis will use a design-to-fabrication-to-testing workflow that combines digital and physical research.

## Sourcing material

Timber waste will be sourced from LSU campus operations, Baton Rouge businesses, and regional manufacturers when possible. Priority will be given to offcuts with dimensions appropriate for repeatable early studies.

## Catalog material

Offcuts will be measured and logged by length, width, height, species if known, visual defects, and source. Initial cataloging may begin with manual measurement in a spreadsheet, with later comparison to faster capture methods if time allows.

## Generate assemblies digitally

The Spruce Beetle workflow developed by Reisach will be used as a base for digital placement and joint generation. In the ETH research, the algorithm was compiled as a Rhino3D/Grasshopper plugin and made publicly accessible with example files, allowing offcuts from a CSV file to be placed along lines or curves through numerical matching and vector-based spatial localization. That makes the plugin especially important to this thesis, because it is not only a precedent but also a tool that can be directly tested, adapted, and extended.

A major part of the methods will therefore be workflow development alongside physical prototyping. Rather than building a completely new system, this project will use the existing Grasshopper workflow as a base and extend it in ways that respond directly to the gaps identified in the ETH paper. Possible areas of development include:

- adapting the placement logic for column and wall systems

- generating multi-sided joints more appropriate for column assemblies and wall-like aggregations

- allowing the width or section of an offcut to help determine how many tenons are generated

- creating more flexible custom joint generation from simple lines, profiles, or member rules

- improving part labeling, sequencing, and data output for easier fabrication and assembly

## Fabricate specimens and prototypes

Selected joints will be generated then cut on the lab CNC. Early work will focus on small test specimens to verify fit, tolerance, and assembly logic. Later iterations will scale to medium prototypes and then to larger demonstrators if time allows. A faux offcut assembly of more standardized pieces may need to be developed in order to reduce the randomness that true offcuts introduce and to make testing results more comparable between iterations.

## Physically test joints and assemblies

Physical testing will focus first on compression-oriented behavior and other basic performance comparisons appropriate to the chosen prototypes. Testing should document:

- maximum load

- deformation and sag

- slip or tolerance accumulation

- splitting behavior

- effect of joint count

- effect of joint geometry

- assembly time

## Evaluate outcomes

Results will be compared against published timber values where appropriate, but the main goal is comparative performance between joint iterations and workflow decisions.

# JOINT AND MATERIAL STUDY FRAMEWORK

## Terminology note

For clarity, this proposal refers to the inserted wood connectors in the Reisach et al. workflow as floating tenons or floating tenon-type joints. Reisach refers to the tested connectors as “loose spline joints,” but in this thesis I will use floating tenon terminology because the connectors are being discussed as discrete inserted joint elements rather than as thin continuous splines running the length of a joint. When necessary, I will note the original wording used in the source paper.

## Joint investigations

The initial focus should remain on timber-only joints that can be simply machined, repeated, and tested.

The joint set begins with the floating tenon baseline established by Reisach and expands into iterations that address what the precedent leaves unresolved: how joint count findings translate to compression-focused assemblies, whether modified geometry can reduce the splitting behavior the paper observed, and whether supplemental locking strategies not explored in that work offer useful gains. The goal is a rational sequence of experiments that can guide later iterations based on findings rather than assumptions.

| Joint type | Status | Likely structural behavior | Main research value |
| --- | --- | --- | --- |
| Floating tenon (called a loose spline in Reisach) | Confirmed in Reisach | Good for alignment and load transfer; limited by splitting and tolerance issues | Baseline for all comparisons |
| Increased number of floating tenons per joint | Suggested by Reisach | Improved stiffness and force distribution | Tests scaling and redundancy |
| Scaled floating tenon geometry | Suggested by Reisach | Better proportional behavior in larger members | Tests dimension-to-capacity relationship |
| Shallower tenon geometry | Proposed | May reduce wedge action and splitting | Tests failure mitigation |
| Dovetail-inspired joint | Proposed | Increased mechanical interlock, stronger resistance to withdrawal | Tests more complex joinery under compression and secondary tension |
| Asymmetrical interlocking profile | Proposed | Could tune insertion direction and bearing behavior | Tests custom responses to irregular offcuts |
| Dowels or wedges for supplemental locking | Proposed | Could improve seating, reduce slip, and add mechanical locking after assembly | Tests secondary locking strategies for tenon-based joints |
| Multi-sided column joint logic | Proposed | Better suitability for stacked or clustered column assemblies | Extends workflow beyond arch conditions |

## Joint matrix and applicable scale

This matrix is preliminary and intended to guide experiment selection.

| Joint type | Small test specimens | Medium prototypes | Full-size demonstrator | Compression suitability | Tension/shear suitability | Fabrication complexity |
| --- | --- | --- | --- | --- | --- | --- |
| Single floating tenon | Yes | Limited | No | Moderate | Low to moderate | Low |
| Double floating tenon | Yes | Yes | Possible | Good | Moderate | Low |
| Triple / quadruple floating tenon | Yes | Yes | Yes | Good to very good | Moderate | Low |
| Floating tenon with increased depth | Yes | Yes | Possible | Good | Moderate | Low |
| Shallower floating tenon | Yes | Yes | Possible | Moderate to good | Moderate | Low |
| Dovetail-inspired joint | Yes | Yes | Possible | Good | Good | Low |
| Asymmetrical interlocking joint | Yes | Yes | Experimental | Unknown but promising | Unknown | High |
| Dowels or wedges for supplemental locking | Yes | Yes | Possible | Good as a secondary aid | Moderate to good | Moderate to high |
| Multi-sided column node / joint set | No | Possible | Yes | Very promising for columns | Unknown | Moderate to high |

## Application to engineered wood products

This matrix identifies how the joint research could translate across waste streams. These are working hypotheses to be tested, not final conclusions.

| Material stream | Waste form | Likely compatibility with proposed workflow | Notes |
| --- | --- | --- | --- |
| Solid sawn timber offcuts | Short rectangular offcuts | Very high | Closest to Reisach precedent |
| Glulam offcuts | Dimensionally stable engineered pieces | High | Good fit for stacked compression assemblies |
| DLT offcuts | Dimensionally stable engineered pieces | High | Good fit for stacked compression assemblies |
| CLT offcuts | Dimensionally stable engineered pieces | High | Good fit for stacked compression assemblies |
| LVL offcuts | Dense engineered strips | Moderate to high | Promising for precise machined joints, but anisotropy and veneer behavior must be considered |
| Irregular logging scraps / organic forms | Non-uniform geometry | Low initially, higher with advanced scanning | Long-term extension of the workflow |

# PROPOSED EXPERIMENTS

## Experiment set 1: baseline joint replication

Replicate the inserted floating tenon logic used by Reisach as closely as possible in order to establish a baseline for fit, fabrication time, and structural behavior.

## Experiment set 2: joint quantity study

Compare one-, two-, three-, and four-tenon configurations to test whether increased joint count improves structural performance and reduces stress concentration.

## Experiment set 3: geometry refinement study

Test adjusted geometries such as:

- shallower tenons

- dovetail-derived forms

- asymmetrical interlocking profile

- dowels or wedges for supplemental locking

- multi-sided column joint

## Experiment set 4: structure study

Develop simple planar arches first and then later column assemblies (if software experiments are successful) using selected joints in order to compare:

- simple arch-based segments

- column sections

# SIGNIFICANCE AND ANTICIPATED CONTRIBUTIONS

Research on circular timber construction has established that digitally fabricated wood-wood assemblies from waste are feasible and that keeping wood in reusable, cascading applications has real environmental value. At the same time, the literature makes clear that wider adoption is held back by limited design guidance, insufficient comparative data on joint behavior, and the absence of integrated workflows for handling unique reclaimed elements (Gamerro et al., 2020; Höglmeier et al., 2015; Reisach et al., 2024). Reversible and interlocking timber connections are well suited to circular construction goals, but their broader use still depends on systematic physical validation and fabrication-aware design development (Churkina et al., 2020; Dissanayake & Gunawardena, 2025).

This thesis contributes to that gap by comparing timber-only joints for offcut-based assemblies, extending a computational workflow from planar demonstrators toward compression-focused prototypes, and identifying software extensions that better support joint variation, fabrication planning, and practical assembly generation (Reisach et al., 2024; Rebstock et al., 2015). The goal is not a single optimized detail, but a tested framework for selecting, producing, and evaluating reusable timber assemblies under real fabrication constraints, one that future work can build on rather than having to reconstruct from scratch (Arsova et al., 2022; Gamerro et al., 2020; Ganeshan et al., 2025).

# CONCLUSION

Timber offcuts represent an underused structural resource, and the primary barrier to using them is not material quality but the absence of a practical, flexible, and validated workflow. This thesis addresses that barrier directly by combining joint development, computational workflow extension, and physical testing in a sequence designed to build toward more complex assemblies as confidence in each component grows. Beginning with simple planar arches and moving toward compression-focused column systems keeps variables manageable early while retaining the broader goals of material reuse and circular construction practice.

A successful outcome would not be a single proven solution, but a tested framework that makes the next phase of this research, and the work of others building on it, more grounded and more practical. The aim is that future researchers and practitioners begin from tested ground rather than assumption.

# REFERENCES

Arsova, S., Genovese, A., & Ketikidis, P. (2022). Implementing circular economy in a regional context: A systematic literature review and a research agenda. Journal of Cleaner Production. https://doi.org/10.1016/j.jclepro.2022.133117
Buren, N. V., Demmers, M., Heijden, R. V. D., & Witlox, F. (2016). Towards a Circular Economy: The Role of Dutch Logistics Industries and Governments. Sustainability, 8, 647. https://doi.org/10.3390/su8070647

Churkina, G., Organschi, A., Reyer, C. P. O., Ruff, A., Vinke, K., Liu, Z., Reck, B. K., Graedel, T. E., & Schellnhuber, H. J. (2020). Buildings as a global carbon sink. Nature Sustainability. https://doi.org/10.1038/s41893-019-0462-4

Dissanayake, H., Gunawardena, T., & Mendis, P. (2025). Adaptation of Connection Systems for Integration with Engineered Wood Products in Buildings: A Systematic Review. Buildings. https://doi.org/10.3390/buildings15071131

Gamerro, J., Bocquet, J., & Weinand, Y. (2020). Experimental investigations on the load-carrying capacity of digitally produced wood-wood connections. Engineering Structures. https://doi.org/10.1016/j.engstruct.2020.110576

Ganeshan, A., Fleischer, K., Jakob, W., Shamir, A., Ritchie, D., Igarashi, T., & Larsson, M. (2025). MiGumi: Making Tightly Coupled Integral Joints Millable. ACM Transactions on Graphics (TOG), 44, 1 - 14. https://doi.org/10.1145/3763304

Han, L., Kutnar, A., Sandak, J., Šušteršič, I., & Sandberg, D. (2023). Adhesive-and Metal-Free Assembly Techniques for Prefabricated Multi-Layer Engineered Wood Products: A Review on Wooden Connectors. Forests. https://doi.org/10.3390/f14020311

Höglmeier, K., Steubing, B., Weber-Blaschke, G., & Richter, K. (2015). LCA-based optimization of wood utilization under special consideration of a cascading use of wood. Journal of environmental management, 152, 158-70 . https://doi.org/10.1016/j.jenvman.2015.01.018

Ilgın, H. E., Karjalainen, M., & Koponen, O. (2021). Review of the Current State-of-the-Art of Dovetail Massive Wood Elements. Engineered Wood Products for Construction [Working Title]. https://doi.org/10.5772/intechopen.99090

Jahan, I., Zhang, G., Bhuiyan, M., & Navaratnam, S. (2022). Circular Economy of Construction and Demolition Wood Waste—A Theoretical Framework Approach. Sustainability. https://doi.org/10.3390/su141710478

Mair-Bauernfeind, C., & Stern, T. (2017). Cascading Utilization of Wood: a Matter of Circular Economy?. Current Forestry Reports, 3, 281-295. https://doi.org/10.1007/s40725-017-0067-y

Moradei, J., Brütting, J., Fivet, C., Sherrow-Groves, N., Wilson, D., Fischer, A., Ye, J., & Cañada, J. (2018). Structural Characterization of Traditional Moment-Resisting Timber Joinery.

Rebstock, F., Bomark, P., & Sandberg, D. (2015). MAKERJOINT, A NEW CONCEPT FOR JOINING MEMBERS IN TIMBER ENGINEERING – STRENGTH TEST AND FAILURE ANALYSES. PRO LIGNO.

Reisach, D., Schütz, S., Willman, J., & Schneider, S. (2024). Digital Fabrication for Circular Timber Construction: A Case Study. Circular Economy. https://doi.org/10.55845/vwgd7873

Tannert, T. (2016). Improved performance of reinforced rounded dovetail joints. Construction and Building Materials, 118, 262-267. https://doi.org/10.1016/j.conbuildmat.2016.05.038